花岗石检测平台     Granite Inspection Plate

Granite Granite Inspection Plate Details

- Place of Origin: Shen Zhen, China (Mainland)

- Brand Name: Hua An Brand

- Material: Natural Black Granite

- Accuracy class: Grade00， Grade0，  Grade1， Grade2；

- Flatness test by: Electronic Level Meter

- Test Standard: According to DIN/JIS/GB

- Packaging & Delivery

Packed with Delicate Poly-wooded Case ; Ply-Wooden case form large size

Delivery time: from one week to one month or more

Product Specialty:

- Made of high quality Natural Black Granite

- High precision and high stability.

- No rust and anti-corrosion.

- Non magnetization.

- Good abrasion resistance.

Physical Property of Natural Black Granite:

- Specific Gravity:         3.03 g/cm3

- Shore Hardness:          > 70Hs-80Hs

- Tensile strength:          211Kg/cm2

- Compressive Strength:         245-254Mpa

- Linear Expansion Coefficient: 4.61´10--6/°C

- Elastic Modulus:                 30-50Gpa

- Water Absorptive:           ≤0.13%

Product Application:

- Mainly used as detection for an important auxiliary tool in the measurement of the platform;

- Important tool to verify difference or tolerance of products against flateness!.

There are some common measurements as the following

| Specifications 规格 | Plateness Tolerance (μm) 平面度公差 |  |  |  | After-Packing VOL (mm) 包装后体积 | Weight (kg)重量 |
| --- | --- | --- | --- | --- | --- | --- |
|  | Grade 000 | Grade 00 | Grade 0 | Grade 1 |  |  |
| 160x100x50 | 0.8 | 1.5 | 3 | 6 | 270x210x150 | 8 |
| 160x160x50 | 0.8 | 1.5 | 3 | 6 | 270x270x150 | 9 |
| 250x160x50 | 0.9 | 1.8 | 3.5 | 7 | 370x270x150 | 11 |
| 250x250x50 | 0.9 | 1.8 | 3.5 | 7 | 370x370x150 | 13 |
| 300x200x50 | 0.9 | 1.8 | 3.6 | 7 | 410x270x180 | 15 |
| 300x300x70 | 1 | 1.9 | 3.8 | 7.5 | 410x370x200 | 27 |
| 400x250x70 | 1 | 2 | 4 | 8 | 510x470x200 | 30 |
| 400x400x70 | 1.2 | 2.3 | 4.5 | 9 | 528x488x210 | 46 |
| 630x400x100 | 1.3 | 2.5 | 5 | 10 | 740x490x270 | 94 |
| 630x630x100 | 1.3 | 2.5 | 5 | 10 | 750x730x270 | 155 |
| 800x500x100 | 1.4 | 2.7 | 5.3 | 11 | 920x600x280 | 155 |
| 900x600x100 | 1.5 | 2.9 | 5.7 | 11.5 | 1000x660x200 | 200 |
| 1000x630x150 | 1.5 | 3 | 6 | 12 | 1120x740x330 | 335 |
| 1000x750x150 | 1.6 | 3.2 | 6.3 | 12.5 | 1250x950x330 | 398 |
| 1000x1000x150 | 1.8 | 3.5 | 7 | 14 | 1250x1230x330 | 532 |
| 1600x1000x200 | 2 | 4 | 8 | 16 | 1870x1230x370 | 1080 |
| 1600x1600x200 | 2.4 | 4.8 | 9.5 | 19 | 1870x1830x370 | 1730 |
| 2000x1000x200 | 2.4 | 4.8 | 9.5 | 19 | 2270x1230x400 | 1345 |
| 2000x1600x250 | 2.5 | 5 | 10 | 20 | 2310x1830x460 | 2622 |
| 2500x1600x300 | 2.9 | 5.8 | 11.5 | 23 | 2810x1830x510 | 3872 |
| 3000x2000x400 | 3.3 | 6.5 | 13 | 27 | 3350x2230x670 | 7651 |
| No standards |  |  |  |  |  |  |

Grade00=1×(1+d/1000)μm；grade0級=2×(1+d/1000)μm；grade1=4×(1+d/1000)μm；grade2=8×(1+d/1000)μm。(d為對角線mm,測量溫度一般在20±2°C)

备注(Notes): 规格Specifications (mm);精度等级Precision grade 000级;平面度Grade 000 flatness(μm)00级;平面度Grade 00 Flatness(μm) 0级;平面度Grade 0 Flatness(μm)1级;
平面度Grade 1 Flatness(μm) ;Net 净重kg